## Slide 1: Problem №1 Adhesive tape
Made by:
Sapegin Vitaliy
Team of Russia
Notes: ─

## Slide 2: Terms of the problem
Determine the force necessary to remove a piece of adhesive tape from a horizontal surface. Investigate the influence of relevant parameters.

## Slide 3: Plan
Nature of cohesive forces
Parameters
Investigate the dependence on initial pressure
Investigate dependence on square of area
Investigate the dependence on applied force angle
Conclusion

## Slide 4: Parameters
1) surface square
2) angle of force application
3) initial pressure

## Slide 5: Setup
Adhesive tape. sticky side up
Body which is removed from tape
Basket with the weight

## Slide 6: Dependence on pressure
Pressing bars
Adhesive tape. sticky side up

## Slide 7: Dependence the removing force on the initial pressure
Chart: P, kPa
| 15 | 20 | 40 | 50 | 70 | 100 | 260 | 345
 | 2.8 | 3.1 | 3.45 | 3.55 | 3.75 | 3.95 | 3.9 | 3.95

## Slide 8: Explanation

## Slide 9: Dependence the removing force on the area of surface
Chart: S, mm²
| 16.779999999999998 | 47.67 | 91.56 | 196.76999999999998 | 277.45
 | 0.6 | 1.3 | 2.17 | 5.2 | 7.04

## Slide 10: Force necessary to remove 1mm² area.
Force necessary to remove 1mm² area of tape

## Slide 11: Dependence on removal angle

## Slide 12: Dependence the removing force on the application angle
Chart: Angle, degrees
| 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100 | 110 | 120 | 130 | 140
 | 12.5 | 9.61 | 7.36 | 6.85 | 5.52 | 4.53 | 3.94 | 3.05 | 2.54 | 2.45 | 2.11 | 1.96

## Slide 14: Dependence the vertical part of removing force on the application angle
Chart: Angle, degrees
| 140 | 130 | 120 | 110 | 100 | 90 | 80 | 70 | 60 | 50 | 40 | 30
 | 1.27 | 1.61 | 2.26 | 2.36 | 2.9 | 3.9 | 4.46 | 5.18 | 5.3 | 5.6 | 6.1 | 6.265

## Slide 15: Derivation of the formula working area tape
Notes: Обозначить S F

## Slide 16: Maximal distance

## Slide 17: Dependence the working area on the cotangent of application angle
Chart: Ctgα
| 1.7321 | 1.1918 | 0.83910000000000062 | 0.57740000000000002 | 0.36400000000000032 | 0.17630000000000001
 | 232.61 | 226.19 | 207.61 | 200 | 193.47 | 165.22

## Slide 18: Scheme
Adhesive tape
Working glue

## Slide 19
Chart: Ctgα
| 0.17630000000000001 | 0.36400000000000027 | 0.57740000000000002 | 0.8391000000000004 | 1.1918 | 1.7321
 | 221 | 276 | 323 | 384 | 432 | 489
 | 221 | 276 | 323 | 384 | 432 | 489

## Slide 20
Chart: Ctgα
| 0.17630000000000001 | 0.36400000000000021 | 0.57740000000000002 | 0.83910000000000029 | 1.1918 | 1.7321
 | 254 | 276 | 295 | 314 | 336 | 368

## Slide 21: Results and conclusion:
The force increases while the initial pressure rises until the force becomes saturated. In this case, it will remain constant
The force increases linearly while the area increases
The force required to remove the tape increases while the angle decreases
Tape has the working area
Maximal distance between tape and surface found

## Slide 22: References
«Nature: a weekly journal of science»
academic journal “Science “

## Slide 23: задачи
Допол рисунок
Вставка формул индексы
Четко объснения дополнительного иследование
Убрать «в» в графиках
Буквы вместо слов
Рисунок с раб площадью

## Slide 24
Chart: Угол в градусах
| 140 | 130 | 120 | 110 | 100 | 90 | 80 | 70 | 60 | 50 | 40 | 30
 | 1.27 | 1.61 | 2.26 | 2.36 | 2.9 | 3.94 | 4.46 | 5.18 | 5.53 | 5.89 | 6.1 | 6.2

## Slide 26
№ | F , Н | m отр. г | S предм. мм 2
1 | 2,27 | 2.3 | 91,56
2 | 2,09 | 0.3 | 91,56
3 | 2,13 | 2.7 | 91,56
1 | 4,75 | 0 | 153.86
2 | 5,20 | 15 | 153.86
3 | 5,55 | 15 | 153.86
1 | 7,43 | 8.4 | 277,45
2 | 7,04 | 6.6 | 277,45
3 | 6,95 | 1.6 | 277,45

## Slide 27: Зависимость от угла
№ | Угол в градусах | Сила F, Н
1 | 90 | 3,94
2 | 90 | 3,92
3 | 90 | 3,95
1 | 60 | 6,15
2 | 60 | 6,84
3 | 60 | 7,01
1 | 45 | 9,30
2 | 45 | 9,68
3 | 45 | 9,84

## Slide 28
№ | m отр. гр | m отр. Гр | S предм. Мм 2
1 | 100 | 3,3 | 28,26
2 | 110 | 7,7 | 28,26
3 | 105 | 2,7 | 28,26
1 | 153 | 1,3 | 63.585
2 | 150 | 4,3 | 63.585
3 | 160 | 7,7 | 63.585
1 | 210 | 13,3 | 94.985
2 | 240 | 17,7 | 94.985
3 | 220 | 3,3 | 94.985
1 | 310 | 5 | 153.86
2 | 320 | 5 | 153.86
3 | 315 | 0 | 153.86
1 | 860 | 11.6 | 660.185
2 | 875 | 3.4 | 660.185
3 | 880 | 9.4 | 660.185

## Slide 29: Расчеты

## Slide 30: Расчеты

## Slide 31
№ | P, КПа | F, Н
1 | 358,64 | 3,94
2 | 358,64 | 3,92
3 | 358,64 | 3,95
1 | 191,34 | 3,97
2 | 191,34 | 3,89
3 | 191,34 | 3,90
1 | 44,27 | 3,10
2 | 44,27 | 3,01
3 | 44,27 | 3,27